Specifier Note: The information provided below is intended to guide the Architect in developing specifications for products manufactured by PROSOCO, Inc. and should not be viewed as a complete source of information about the product(s). The Architect should always refer to the Product Data Sheet and MSDS for additional recommendations and for safety information.

Specifier Note: Paragraph below is for PART 1 GENERAL, Quality Assurance.

Test Area

Test a representative area of no less than 10 ft. by 10 ft. (and no more than 10% of the total floor area) to confirm surface preparation procedures, coverage rate, reaction time, finished appearance, etc. Use the manufacturers’ application instructions. Let test area dry thoroughly before inspection. Get owner’s approval before proceeding. Keep test area available for comparison throughout the project.

Specifier Note: Paragraphs below are for PART 2 PRODUCTS, Manufacturers and Products.

Manufacturer: PROSOCO, Inc., 3741 Greenway Circle, Lawrence, KS 66046. Phone: (800) 255-4255; Fax: (785) 830-9797. E-mail: CustomerCare@prosoco.com

Product Description

Consolideck® First Cut with Densifier is a water-based blend of surfactants and silicates applied to the concrete surface prior to and during wet-grinding. First Cut with Densifier combines the technologies of surfactants and silicates to perform as both a grinding aid and concrete hardener. The formulation is specially designed to penetrate and react with concrete, leaving a harder and denser surface after grinding. First Cut with Densifier lifts concrete slurry solids away from the surface, suspends them and clears the path for the diamonds. This keeps the slurry solids from interfering with the ability of the diamonds to remove the concrete surface, increasing efficiency. First Cut with Densifier reduces the amount of time spent with each metal and lower grit resin-bound diamond tooling, shortening the overall project timeline and extending the life of the diamonds.

Typical Technical Data

FORM: Clear, water-like liquid

SPECIFIC GRAVITY: 1.05

pH: 11.3

WEIGHT/GALLON: 7.90 pounds

ACTIVE CONTENT: not applicable

TOTAL SOLIDS: not applicable

VOC CONTENT: less than 0.5 percent. Complies with all known national, state and district VOC regulations.

FLASH POINT: greater than 212 degrees F (greater than 100 degrees C)

FREEZE POINT: 32 degrees F (0 degrees C)

SHELF LIFE: 2 years in tightly sealed, unopened container.

Specifier Note: Paragraphs below are for PART 3 EXECUTION, Installation.

Application

Before applying, read “Preparation” in the Manufacturer’s Product Data Sheet and the Safety Data Sheet for Consolideck® First Cut With Densifier. Do not dilute or alter. Apply as packaged. Mix well before use.

SPECIFIER NOTE: Consolideck® First Cut with Densifier should only be used when wet-grinding concrete floors.

SPECIFIER NOTE: The following instructions are guidelines that can be modified for specific equipment, job-site conditions or personal experience.

- Wet concrete surface with water.

- Apply First Cut with Densifier on the floor. Saturate the floor, but do not create puddles.

- Wet-grind the floor starting with lowest grit diamonds specified. Keep floor wet to create thick foam of slurry.

- If floor starts to dry while grinding, re-saturate with water. Do not allow floor to completely dry.

- After each grinding level, clean the floor with fresh water; solution and slurry should be removed/vacuumed up. If thoroughly cleaned, the floor can dry between grinding levels.

SPECIFIER NOTE: If an autoscrubber is used, a commercially available defoamer may be added to the recovery tank.

- Reapply First Cut with Densifier, following steps 1–5 above.

- When finished, remove/vacuum up all solution and slurry. Clean the floor with fresh water, and allow to dry.

Cleanup: Clean tools and equipment using fresh water.